压降电容（X2）电容器

FEATURE（特点）：

1、宽温度、频率范围内，容量和DF具有高稳定性

High stability of capacitance and DF versus wide temperature and frequency range ;

■  高电流承受及高绝缘强度

High transient endurance and high dielectric strength ;

■  长时间工作于严酷环境下（如高温高湿）容量稳定

High stability of capacitance under serving ambient condition(such as high temperature and high humidity);

■  自愈性好，能承受浪涌电压冲击

Excellent self-healing ,withstanding surge-voltage stressing.

APPLICATION（用途）：

■   电源串联连接用 For connection in series with power supply

■   阻容降压用 For capacitive divider power supply

■   线间跨接，抑制电源电磁干扰Across- the-line, Spark killer;

■   开关电源Switching power supply.

SPECIFICATIONS(技术要求)：

| DIELECTRIC 介质 | Polypropylene film 聚丙烯薄膜 |
| --- | --- |
| ELECTRODES 电极 | Vacuum evaporated metal 真空蒸镀金属 |
| COATING 包封 | Encapsulated in reinforced flame retardant plastic case sealed with epoxy resin meeting the requirement of UL94V-0 阻燃盒子并以环氧树脂灌封 |
| LEADS 导线 | Radial leads of tinned wire/insulation flexible wire 径向镀锡导线或软导线 |
| REFERENCE STANDARD 引用标准 | IEC 60384-14,EN60384-14 |
| CLIMATIC CATALOGUE 气候类别 | 40/100/21（GMF） 40/110/21(UL) |
| Capacitance Versus Rated voltage (DC) 静电容量与额定电压 | 0.1uF-2.2 uF/275VAC(50/60Hz)、（UL） |
| CAPACITANCE TOLERANCE 静电容量误差 | M=±20% K=±10% J=±5% |
| Dissipation factor (tangent of loss) 散逸因素(损耗角正切) | DF≤0.1% (at 20℃,1KHz) |
| VOLTAGE PROOF 耐电压 | 4.3*UR Unit:VDC(1 minute at 20℃) |
| Insulation resistance 绝缘电阻 | C≤0.33uF IR≥15000MΩ C ＞0.33uF IR*C≥5000S (1 minute at 20℃ and RH≤65%) |
| Endurance 耐久性 | 85℃实验温度下，125%UR交流电压1000小时，实验过程中，每个电容器串联一个47ῼ电阻。1000V交流电压（60HZ），每一小时施加0.1S，实验完成后： ΔC/C≤10%; ΔC/C≤0.8% (C≤1uF) ΔDF≤0.5%;(C>1uF) IR≥50% of the specified value（标称值） |

OUTLINE DRAWING(外观图)

DIMENSION（尺寸）:                                  Unit（单位）: mm

| SYMBOL | W ±0.5 | H ±0.5 | T ±0.5 | P ±1.0 | D ±0.05 | SYMBOL | W ±0.5 | H ±0.5 | T ±0.5 | P ±1.0 | D ±0.05 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 104 | 18 | 12 | 6 | 15 | 0.8 | 104 | 26.5 | 15 | 6 | 22.5 | 0.8 |
| 124 | 18 | 12 | 6 | 15 | 0.8 | 124 | 26.5 | 15 | 6 | 22.5 | 0.8 |
| 154 | 18 | 12 | 6 | 15 | 0.8 | 154 | 26.5 | 15 | 6 | 22.5 | 0.8 |
| 184 | 18 | 14.5 | 8.5 | 15 | 0.8 | 184 | 26.5 | 15 | 6 | 22.5 | 0.8 |
| 224 | 18 | 14.5 | 8.5 | 15 | 0.8 | 224 | 26.5 | 16 | 7 | 22.5 | 0.8 |
| 274 | 18 | 16 | 10 | 15 | 0.8 | 274 | 26.5 | 16 | 7 | 22.5 | 0.8 |
| 274 | 18 | 14.5 | 8.5 | 15 | 0.8 | 274 | 26.5 | 16 | 7 | 22.5 | 0.8 |
| 334 | 18 | 18 | 10 | 15 | 0.8 | 334 | 26.5 | 17 | 8.5 | 22.5 | 0.8 |
| 334 | 18 | 16 | 10 | 15 | 0.8 | 334 | 26.5 | 16 | 7 | 22.5 | 0.8 |
| 394 | 18 | 16 | 10 | 15 | 0.8 | 394 | 26.5 | 17 | 8.5 | 22.5 | 0.8 |
| 474 | 18 | 18 | 10 | 15 | 0.8 | 474 | 26.5 | 18.5 | 10 | 22.5 | 0.8 |
| 564 | 18 | 18 | 10 | 15 | 0.8 | 564 | 26.5 | 18.5 | 10 | 22.5 | 0.8 |
| 684 | 18 | 18 | 10 | 15 | 0.8 | 684 | 26.5 | 18.5 | 10 | 22.5 | 0.8 |
|  |  |  |  |  |  | 824 | 26 | 21.5 | 12 | 22.5 | 0.8 |
|  |  |  |  |  |  | 105 | 26.5 | 23 | 14 | 22.5 | 0.8 |
|  |  |  |  |  |  | 105 | 26 | 21.5 | 12 | 22.5 | 0.8 |
|  |  |  |  |  |  | 125 | 32 | 22 | 13 | 27.5 | 0.8 |
|  |  |  |  |  |  | 155 | 31 | 25 | 14 | 27.5 | 0.8 |
|  |  |  |  |  |  | 185 | 31 | 25 | 14 | 27.5 | 0.8 |
|  |  |  |  |  |  | 225 | 31 | 25 | 14 | 27.5 | 0.8 |

SAFETY APPROVALS（认证通过文件及引用标准）

|  | UL60384—14 | E152288 E221606 |
| --- | --- | --- |
|  | VDE (EN60384-14) | 40000463 |
|  | VDE(EN60384-14) EN/EC | 40000463 |
|  | CQC（GB/T14472-98） | CQC03001002847 |
|  | CB（IEC60384-14） | DE1-49036 |
|  | KC（K60384-14） | SU03035-7001A SU03035-7002A SU03035-7003A |